NiMH BATTERY CHARGING/DISCHARGING INSTRUCTIONS

| CAPACITY | STANDARD TRICKLE CHARGE | MAX PEAK CHARGE RATE | MAX DISCHARGE RATE |
| --- | --- | --- | --- |
| 160mah 1/3 AAA | 16ma ~ 14-16 hours | 160mA | 480 mA |
| 400mah 2/3 AAA | 50ma ~ 7-8 hours | 400mA | 1200 mA |
| 730mah AAA | 100ma ~ 8-9 hours | 500mA | 1 Amp |
| 1000mah AAA | 100ma ~ 11-12 hours | 500mA | 1 Amp |
| 250mah 1/3 AA | 25ma ~ 14-16 hours | 250mA | 750 mA |
| 700mah 2/3 AA | 100ma ~ 7-8 hours | 500mA | 1 Amp |
| 850mah FLAT | 100ma ~ 10-11 hours | 500mA | 3 Amps |
| 1100mah 2/3 A | 100ma ~ 12-13 hours | 500mA | 3 Amps |
| 1200mah 2/3 A | 100ma ~ 13-14 hours | 500mA | 3 Amps |
| 1300mah 2/3 A | 100ma ~ 13-14 hours | 500mA | 3 Amps |
| 1500mah 2/3 A | 100ma ~ 16-17 hours | 1.0 Amp | 30 Amps |
| 1400mah AA | 100ma ~ 15-16 hours | 1.0 Amp | 15 Amps |
| 1700mah AA | 100ma ~ 18-19 hours | 1.0 Amp | 20 Amps |
| 2000mah 4/5 A | 150ma ~ 13-15 hours | 1.5 Amps | 30 Amps |
| 2150mah 4/5 A | 150ma ~ 14-16 hours | 1.5 Amps | 10 Amps |
| 2600mah AA | 100ma ~ 28-29 hours | 500mA | 5 Amps |
| 2700mah A | 100ma ~ 26-27 hours | 1.5 Amps | 10 Amps |
| 4200mah sub-C | 420ma ~ 11-13hours | 3.0 Amps | 35 Amps |
| 4500mah sub-C | 450ma ~ 11-13hours | 3.0 Amps | 35 Amps |
| 4000mah 4/3 A | 500ma ~ 9-10hours | 2.0 Amps | 10 Amps |
| 5000mah C | 500ma ~ 11-12 hours | 3.0 Amps | 20 Amps |
| 10000mah D | 600ma ~ 14-16 hours | 3.0 Amps | 20 Amps |

**Calculate your charge time: Battery Capacity +10% / Charger output = hours charge time

NiMH Battery Pack Maintenance

- If you are having trouble charging your NiMH battery pack –trickle charge at 1/10 C (capacity) to wake them up and reach full capacity. This also applies to packs that have been in storage.

- Trickle charge time listed in the chart above is for fully discharged packs.

Always let the batteries cool to room temperature before charging. Heating your NiMH battery pack up beyond 110 F degrees indicates an overcharge condition and will lead to cell damage, loss of voltage and capacity.

3.) Nickel-Metal Hydride cells are more sensitive to heat than Nicads, so be sure not to overcharge them. Overcharging may cause the cells to vent and loose capacity. It is recommended that you charge with a charger that has an adjustable Delta Peak detection circuit (set to .01-.02v) eliminating the possibility of overcharging. Nickel-Metal Hydride cells will quickly get hot after the voltage starts dropping, so keep track of the time on the charger.

4.) NiMH vs. NiCad; Although Nicad batteries give higher average voltage numbers when tested on matching Machines, this is due to NiCads having a high initial “peak” voltage which burns away quickly within the first minute. The Nickel-Metal Hydride cells actually carry more usable voltage over the entire discharge cycle. You will notice that the NiMH cells will have more punch later in the discharge cycle than NiCads.

5.) Store your NiMH with some voltage left in them. Do not dead short them, or store them on a resister.

6.) Charging 2 packs at the same time with one charger: Both packs must be identical voltage, chemistry and mah.

Both packs must be completely discharged to .85 volts per cell before charging.

7.) If you wish to discharge your NiMH batteries discharge to no less than .85 volts per cell.